High Power Laser Diode

Specifications:

| parameter | Units | 793mm | 880mm | 940mm | 1.64mm |
| --- | --- | --- | --- | --- | --- |
| continuous output power(P) | W | 3 | 5 | 2 | 4 | 2.5 |
| Light-emitting area | um | 100*1 | 150*1 |
| operating wavelength (λc) | nm | 790±3 | 880±5 | 940±10 | 1060±5 |
| spectral width (Δλ) | nm | ≤2 |
| Working current (Io) | A | ≤4.1 | ≤4.8 | ≤2.5 | ≤4.1 | ≤3.0 |
| Working Voltage(Vf) | V | ≤2.3 |
| Threshold Current(Ith) | A | ≤0.70 | ≤0.90 | ≤0.5 | ≤0.35 | ≤0.3 |
| slope efficiency(Es) | W/A | >1.0 |
| differential resistance (Rd) | Ω | ≤0.2 |
| photoelectric conversion efficiency | % | >50% |
| Beam Divergence ( θ⊥×θ∥) | ° | <40×10 |
| life expectancy | h | ≥10,000 |
| Package Type |  | TO3/C-mount |

Packaging and Dimensions:

Special remind:

- (1)C - Mount encapsulation，the electrode lead is negative，the tube is positive

- TO3 encapsulation，Ceramic pin is negative，the tube is positive

Precautions:

- When the laser work, avoid eye and skin in laser irradiation

- anti-static measures must be taken when using and transportation and storage,During transportation and storage,the short line protection is need to connected between pins.

- Using the constant current power supply, avoid surge at work

- Should be used under the rated current rating rated current and rated power.

- Need to ensure good thermal when the laser work.

(6)Optimum working temperature is 25 ℃

(7)Storage temperature :-20 ℃ ~ +60 ℃